## Slide 1: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
1 | Introduction
2 | Electrostatic and thermodynamic potentials of electrons in materials
3 | Voltage, capacitance and batteries
4 | Work functions and injection barriers
5 | Thermal distribution of electrons, holes and ions in solids
6 | Interfacial kinetics and hopping transitions
7 | The chemical capacitance
8 | The density of states in amorphous solids
9 | Planar and nanostructured semiconductor junctions

## Slide 2: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
This book analyses the fundamental concepts, main properties and key applications, of energy devices that are made using nanostructured materials, including hybrid and organic solar cells, electrochemical batteries, diodes, LEDs and OLEDs, transistors, and the direct conversion of solar radiation to chemical fuels.
The book is mainly devoted to the physical and electrochemical properties of devices, from molecular aspects to macroscopic models.
We treat a broad class of devices that typically use electrochemical setups, thin films, and organic materials, normally formed by solution processed routes for low cost applications.

## Slide 3: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Energy devices
Sunlight and water are in effect inexhaustible resources to provide the required diversity of energy supplies. Sunlight striking the earth comprises the largest energy resource base currently available.
Conversion of solar photons into a usable form of energy is a big challenge
Electricity, fuels and storage
Chapter 1
Introduction

## Slide 4: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
“A system far removed from its condition of equilibrium is the one chosen if we wish to harness its processes for the doing of useful work”
[G. N. Lewis and M. Randall, Thermodynamics, 1923, p. 111].
unidirectional flow of all systems toward the final state of equilibrium
Battery, voltage
Solar cell, out of equilibrium
the cornerstone of energy devices is to find an effective way to channel processes in a given direction and avoid reciprocal processes that constitute a waste

## Slide 5: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Fig. 1.1 Top view micrographs of mesoporous films composed by different nanostructured metal oxides deposited on transparent conducting substrates: (a) TiO2 nanoparticles, 250 nm particle size, (b) WO3 nanoparticles processed by hydrothermal synthesis (c) Fe2O3 deposited by spray pyrolysis. Courtesy of Sixto Giménez.

## Slide 6: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Fig. 1.2 SEM image of the cross section of a porous electrode formed by sintered TiO2 anatase crystals (inset), deposited on a transparent substrate that consists on a glass support and thin TCO layer. Courtesy of Ronen Gottesman and Arie Zaban.

## Slide 7: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 1.3. Atomic structure of anatase TiO2 nanocrystal. Adapted from Nunzi, F.; Mosconi, E.; Storchi, L.; Ronca, E.; Selloni, A.; Gratzel, M.; De Angelis, F. "Inherent electronic trap states in TiO2 nanocrystals: effect of saturation and sintering". Energy & Environmental Science 2013, 6, 1221-1229, with permission.
SEM pictures of nanostructured TiO2 electrodes, courtesy of Eric Diau

## Slide 8: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Fig. 1.4. Scheme of electron transport in a metal oxide nanostructure, showing a photogeneration event, and the density of states in the semiconductor bandgap. Courtesy of Juan A. Anta and José P. González.
Fig. 1.5. Scheme of electron transport in a metal oxide nanostructure, showing a photogeneration event, and the density of states in the semiconductor bandgap. Courtesy of Juan A. Anta and José P. González.

## Slide 9: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Fig. 1.6 Scheme of solar energy conversion scheme using nanoheterostructures.

## Slide 10: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 1.7. (a) Scheme of nanostructure that carries electrons and holes in different phases. (b) The structure of bulk heterojunction solar cells, with two organic phases closely mixed and separately interconnected. (c) Energetic scheme of a dye-sensitized solar cell, showing the absorber dye molecule between electron transport material, and hole transport material, and (d) the energetic disorder in recombination process. (e) Energetic scheme of a bulk heterojunction solar cell, with carrier generation in both fullerene PCBM and polymer P3HT, and (f) the energetic disorder in recombination process. (g) Generation and charge transfer in a quantum dot sensitizer.

## Slide 11: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Device understanding usually consists on a picture of how the device operates internally that is sufficient for rationalizing the outcome of different manipulations that can be performed.
Such understanding is based in a broad range of physical principles, on a comprehension of different classes of materials and their interfaces, and on the mastering of chemical features of molecules.